## Slide 1: Lecture 1: Reciprocal Lattice, Covariant and Contravariant Tensors

## Slide 2: 1. Review of the Reciprocal Lattice

## Slide 3: What is the Reciprocal Lattice?
A fundamental mathematical construct in materials science.
Crucial for understanding:
  X-ray/Electron Diffraction
  Electronic Band Structure (Solid-State Physics)
Provides a framework for analyzing wave-particle interactions in periodic crystal structures.

## Slide 4: Definition of Reciprocal Lattice Basis Vectors
Real-space primitive basis vectors: $ _1, _2, _3 $$
Reciprocal-space primitive basis vectors: $ ^*_1, ^*_2, ^*_3 $$
Defining Orthonormalization Condition:
  $ _{ij}
  $$ is the Kronecker delta (1 if $ i=j $$
  , 0 if $ i j $$).
  $ 2$$ factor is common in physics (sometimes omitted in crystallography).
Explicit Formulas:
(and cyclic permutations for $ ^*_2, ^*_3
$$) * $ V = \mathbf{a}_1 \cdot (\mathbf{a}_2 \times \mathbf{a}_3) $$
is the volume of the real-space primitive unit cell.

## Slide 5: Key Properties:
Orthogonality: Each $ ^*_i
$$ is perpendicular to the *other two* real-space basis vectors. * Example: $ \mathbf{a}^*_1 \perp \mathbf{a}_2 $$
and $ ^*_1 _3 $$.
Magnitude: $ |^*_i| $$ is inversely proportional to the spacing of the real-space lattice planes to which it is normal.
Angle (for orthogonal systems): Angle between $ ^*1 $$ and $ \mathbf{a}^*_2 $$ is $ 180^- {12} $$.
Qualitative Visualization: Helpful for intuition, but exact calculations require the mathematical definitions.

## Slide 6: Constructing Reciprocal Lattice Points & The Uniqueness Issue
Reciprocal lattice points: $ _{hkl} = h ^*_1 + k ^*_2 + l ^*_3
$$ ($ h,k,l $$
are integers).
Apparent Problem: The choice of real-space primitive cell is not unique, leading to different sets of primitive reciprocal basis vectors.
Resolution: The reciprocal lattice is fundamentally determined by the set of all real-space lattice points and their underlying periodicity.
  This non-uniqueness is resolved by considering extinction rules.

## Slide 7: 2. Physical Significance

## Slide 8: The Reciprocal Lattice as a Fourier Transform
Reciprocal lattice points $
$$ are the wave vectors for which a plane wave $ e^{i \mathbf{G} \cdot \mathbf{r}} $$
has the crystal’s periodicity.
Scattering Theory: The scattered wave amplitude $ S()
$$ is the Fourier transform of the electron density $ \rho(\mathbf{r}) $$
.
Bragg’s Law / Laue Condition: Constructive interference (diffraction peaks) occurs when the scattering vector $
$$ equals a reciprocal lattice vector $ \mathbf{G} $$
.
(Equivalent to $ 2d = n$$)
Physical Meaning: Only reciprocal lattice points corresponding to non-zero scattering amplitudes have physical significance.

## Slide 9: Extinction Rules (Selection Rules)
Arise from internal symmetries (e.g., centering atoms, screw axes, glide planes).
Lead to destructive interference, “extinguishing” certain diffraction peaks/reciprocal lattice points.
Crucial for Reciprocal Lattice Uniqueness:
  Applying extinction rules ensures a unique physically relevant reciprocal Bravais lattice.
  Example: A real-space Face-Centered Cubic (FCC) lattice has extinction rules ($ h,k,l $$ must be all even or all odd) that result in a Body-Centered Cubic (BCC) reciprocal lattice.

## Slide 10: Correspondence: Real vs. Reciprocal Bravais Lattices
Real-Space Lattice | Reciprocal Lattice
Simple Cubic (SC) | Simple Cubic (SC)
Body-Centered Cubic (BCC) | Face-Centered Cubic (FCC)
Face-Centered Cubic (FCC) | Body-Centered Cubic (BCC)
Simple Hexagonal (SH) | Simple Hexagonal (SH)

## Slide 11
Key Duality: BCC and FCC lattices are reciprocal duals of each other.
Visualization: Tools like crystaldrawcell.py help understand these transformations.

## Slide 12: 3. Covariant and Contravariant Tensors

## Slide 13: Lattice Transformation Rules Revisited
How do physical quantities transform when the coordinate system (basis vectors) changes?
Real-space basis vectors: $ ’_i = j T{ij} _j $$
Real-space coordinates: $ x’^i = j (T^{-1}){ji} x^j $$
Reciprocal-space basis vectors: $ ’^*_i = j (T^{-1}){ji} ^*_j $$
Reciprocal-space coordinates (Miller indices): $ h’^i = j T{ij} h^j $$

## Slide 14: Defining Covariant and Contravariant Vectors
Covariant Vectors (co-vary): Components transform in the same way as the basis vectors ($
$$). * Examples: Real-space basis vectors ($ \mathbf{a}_i $$
), Reciprocal-space coordinates ($ h_i
$$). * Often denoted with **subscripts** ($ V_i $$
).
Contravariant Vectors (contra-vary): Components transform in the inverse transpose way relative to basis vectors ($ ^{-1}$ or $ ({-1})T
$$). * Examples: Real-space coordinates ($ x^i $$
), Reciprocal-space basis vectors ($ ^i
$$ or $ \mathbf{a}^*_i $$
).
  Often denoted with superscripts ($ V^i $$).
Historical context: Formalized by Albert Einstein for general relativity, ensuring physical laws are independent of coordinate choice.

## Slide 15: The Metric Tensor
A fundamental tensor that encodes the geometry of space (measures lengths, angles).
**Real-space metric tensor ($ g_{ij}
g_{ij} = _i _j
$$ * Transforms with two factors of $ \mathbf{T} $$
Second-rank covariant tensor.
**Reciprocal-space metric tensor ($ g^{ij}
g^{ij} = ^*_i ^*_j
$$ * Transforms with two factors of $ \mathbf{T}^{-1} $$
Second-rank contravariant tensor.
Crucial Relationship: The real-space and reciprocal-space metric tensors are matrix inverses of each other (up to a scalar factor).

## Slide 16: Relation Between Real-Space & Reciprocal-Space Transformations
The fundamental definition: $ ^*_i j = 2{ij} $$
This implies that the matrix of reciprocal basis vectors is proportional to the inverse transpose of the matrix of real-space basis vectors:
Metric Tensors as Converters: They bridge covariant and contravariant components.
  Lowering an index: $ X_i = g_{ij} X^j $$
  Raising an index: $ X^i = g^{ij} X_j $$

## Slide 17: Invariance of Scalar Products
The dot product of a covariant vector and a contravariant vector (with contracted indices) is always an invariant scalar quantity.
  The length (norm) of a vector does not change just because we change our coordinate system.
This is a cornerstone of physics: physical quantities and laws must be independent of the chosen coordinate system.

## Slide 18: Einstein Summation Convention
Rules for Index Placement:
  Covariant indices: Subscripts ($ A_i $$).
  Contravariant indices: Superscripts ($ A^i $$).
Implied Summation (Contraction): If an index appears exactly once as a subscript and once as a superscript in a single term, summation over that index is implied.
Benefits:
  Conciseness: Equations are much shorter.
  Clarity on Invariance: Contractions (summing over one upper and one lower index) always yield scalar invariants.
  Consistency Check: In a valid tensor equation, free indices (not summed over) must match in position and type on both sides.

## Slide 19: Covariance of Physical Equations
An equation is covariant if its form remains unchanged under coordinate transformations.
In tensor notation, this means the index structure (number and position of upper/lower indices) must be identical on both sides of the equation.
Connection to Symmetry: Physical laws are often required to satisfy fundamental symmetries (e.g., translational, rotational, Lorentz invariance). Expressing them as covariant tensor equations ensures these symmetries are respected.
Examples:
  Maxwell’s equations (Lorentz covariant).
  Einstein’s field equations (generally covariant under arbitrary coordinate transformations).

## Slide 20: Identifying Unknown Tensor Components
The index rules allow us to deduce the covariant or contravariant nature of unknown tensors.
Example: Basis vector transformation: $ ’_i = T^j_i _j
$$ * $ \mathbf{a}_i $$
(covariant), $ _j
$$ (covariant). The sum is over $ j $$
.
  Therefore, the transformation matrix $ T^j_i
  $$ must be a **mixed tensor of rank 2** (one contravariant index $ j $$
  , one covariant index $ i $$).
Examples in Materials Science:
  Dielectric permittivity tensor $ _{ij} $$: Second-rank covariant.
  Strain tensor $ _{ij} $$: Second-rank covariant.
  Elastic constant tensor $ C_{ijkl} $$: Fourth-rank covariant.

## Slide 21: Tensor Components in Cartesian vs. Crystallographic Coordinates
Crystallographic Coordinates: Based on the crystal’s primitive lattice vectors; natural for anisotropic properties of single crystals.
Cartesian Coordinates: Mutually orthogonal axes; often used in computational materials science (e.g., VASP output).
  Simplifies tensor algebra ($ g_{ij} = _{ij} $$).
  Provides a universal reference frame for comparison.
VASP Example: Defines Cartesian axes based on the lattice vectors in the POSCAR file. Outputted tensor components are in this Cartesian system.
  Requires coordinate transformation to interpret in crystallographic directions.

## Slide 22: Summary of Covariant and Contravariant Rules
Basis Vectors vs. Coordinates:
  Covariant basis vectors $ _i
  $$ pair with contravariant coordinates $ x^i $$
  .
  Contravariant basis vectors $ ^i
  $$ pair with covariant coordinates $ x_i $$
  .
  $ = x^i _i = x_i ^i $$
Real Space vs. Reciprocal Space:
  Real-space basis vectors $ _i $$ are covariant.
  Reciprocal-space basis vectors $ ^i $$ are contravariant.
Differentiation: Derivatives can change covariance/contravariance.
  $ $$ (gradient wrt contravariant coord) is covariant.
Metric Tensor ($ g_{ij} $$, $ g^{ij} $$): Used to “raise” and “lower” indices (convert between covariant and contravariant components).
  $ X_i = g_{ij} X^j $$ (lowers index)
  $ X^i = g^{ij} X_j $$ (raises index)

## Slide 23: Geometric Interpretation of Coordinates
Contravariant Coordinates ($ x^i $$):
  Represent components found by parallel projection onto the real-space basis vectors.
  They tell you “how much of each basis vector” is needed to construct the vector.
Covariant Coordinates ($ x_i $$):
  Represent components found by orthogonal projection onto the directions defined by the reciprocal-space basis vectors.
  They relate to the “projection onto the plane normal to the other real-space basis vectors.”
Understanding this geometric duality is key to mastering tensor analysis in materials science.
Thank you!