## Slide 1: Slide 1: Fabrication of Polycrystalline Silicon Thin Films by a Two-Step Growth Method

## Slide 2: Text
Fabrication of Polycrystalline Silicon Thin Films by a Two-Step Growth Method – Controlling Structure and Properties through Surface Reaction Control – (T. Kamiya, K. Nakahata, J. Mitsuida, H. Lu, C. M. Fortmann, I. Shimizu, Tokyo Institute of Technology)

## Slide 3: Outline
Background
Two-Step Growth Method
Experimental Results
  Interface Structure (Ellipsometry)
  Influence of Seed Layer
Summary

## Slide 4: Diagram Text
Substrate Seed crystal poly-Si grain

## Slide 5: Slide 2: Background

## Slide 6: Text
Fabrication of Polycrystalline Silicon Thin Films by PE-CVD Method Using SiF4 Source Gas * Highly crystalline polycrystalline silicon at low temperatures * High deposition rate (~10 Å/s) * High preferred orientation (022)
Deposition on glass substrates: Need to reduce initial amorphous layer * Layer-By-Layer (LBL) Method * Two-Step Growth Method

## Slide 7: Slide 3: Two-Step Growth Method

## Slide 8: Text

## Slide 9: Growth Process
Substrate Epitaxial-like growth Low-temperature deposition (200~350°C) High deposition rate poly-Si

## Slide 10: Seed Layer Process
Substrate Seed crystal (~100nm) High preferred orientation High crystallinity High-temperature deposition (Ts > 360°C) Layer-By-Layer Method

## Slide 11: Slide 4: Previous Work: Impact of Air Exposure

## Slide 12: Text
宮本さんデータ (Miyamoto et al.’s data)
Time (sec) on P-doped poly-Si SiF4 50 sccm SiF4 40 sccm SiF4 30 sccm

## Slide 13: 図
スライド4の図1

## Slide 14
スライド4の図2 スライド4の図3 スライド4の図4 スライド4の図5 スライド4の図6 スライド4の図7 スライド4の図8 スライド4の図9 スライド4の図10 スライド4の図11 スライド4の図12 スライド4の図13 スライド4の図14 スライド4の図15 スライド4の図16

## Slide 15: Slide 5: Objective

## Slide 16: Text

## Slide 17: Objective
To achieve an epitaxial-like interface between the seed layer and the grown polycrystalline thin film in the two-step growth method.
To investigate the influence of the seed layer crystallinity on the final film structure in the two-step growth method.

## Slide 18: Slide 6: Experimental Setup

## Slide 19: Text

## Slide 20: Experimental Setup
Modulator Susceptor MBP (Microwave Plasma) Auto Vacuum Controller Ar/H2 SiF4 Shutter in-situ Spectroscopic Ellipsometer Substrate Light source Controlled by Sequencer Layer-By-Layer Method H2 SiF4 Process time Gas flow Deposition Atomic Hydrogen Treatment Crystallinity Promotion Detector Magnet

## Slide 21: Slide 7: Experimental Method

## Slide 22: Text

## Slide 23: Experimental Method
Structural Evaluation:
Spectroscopic Ellipsometer (SE)
Powder X-ray Diffraction (XRD)
Observation of deposition process:
Ellipsometer ( at 4.15eV)
Typical Deposition Conditions (Table placeholder)

## Slide 24: 図
スライド7の図1

## Slide 25
スライド7の図2

## Slide 26: Slide 8: Evolution of during Growth Process

## Slide 27: Text

## Slide 28: Evolution of during Growth Process
(SiF4/H2 : Same for Seed Layer Process and Growth Process) (Seed: 50/5/30, 380°C - poly-Si: 50/5/30)

## Slide 29: 図
スライド8の図1

## Slide 30: Slide 9: Evolution of during Growth Process

## Slide 31: Text

## Slide 32: Evolution of during Growth Process
(SiF4/H2 : Increased SiF4 flow rate in Seed Layer Process) (Seed: 50/5/60, 380°C - poly-Si: 50/5/30)

## Slide 33: 図
スライド9の図1

## Slide 34: Slide 10: Evolution of during Growth Process

## Slide 35: Text

## Slide 36: Evolution of during Growth Process
(SiF4/H2 : Further increased H2 flow rate in Growth Process) (Seed: 60/5/60, 380°C - poly-Si: 60/10/30)

## Slide 37: 図
スライド10の図1

## Slide 38: Slide 11: Influence of Seed Layer on the Structure of Films Fabricated by Two-Step Growth Method

## Slide 39: Text

## Slide 40: Influence of Seed Layer on the Structure of Films Fabricated by Two-Step Growth Method

## Slide 41: 図
スライド11の図1

## Slide 42: Slide 12: Seed Layer Dependence of Change during Growth Process

## Slide 43: Text

## Slide 44: Seed Layer Dependence of Change during Growth Process
Seed: 60/5/60 Seed: 60/10/60 (poly-Si: 60/10/60)

## Slide 45: 図
スライド12の図1

## Slide 46
スライド12の図2

## Slide 47: Slide 13: Influence of Seed Layer on the Structure of Films Fabricated by Two-Step Growth Method (SE, XRD Comparison)

## Slide 48: Text

## Slide 49: Influence of Seed Layer on the Structure of Films Fabricated by Two-Step Growth Method
Seed: 60/5/60 Seed: 60/10/60 Diffraction intensity / counts (poly-Si: 60/10/60)

## Slide 50: 図
スライド13の図1

## Slide 51
スライド13の図2 スライド13の図3 スライド13の図4

## Slide 52: Slide 14: Summary

## Slide 53: Text

## Slide 54: Summary
Achieved improved and continuous interface structure by controlling gas flow rates in both seed layer and growth processes.
Found that the structure of the seed layer significantly influences the final film structure, especially at lower growth temperatures.