## Slide 1: SLIDE 1: Fabrication of Polycrystalline Silicon Thin Films by a Two-Step Growth Method

## Slide 2: Text
Fabrication of Polycrystalline Silicon Thin Films by a Two-Step Growth Method – Structural Control and Properties through Surface Reaction Control – (Tokyo Institute of Technology) ○Toshio Kamiya, Koichi Nakahata, Atsushi Mitsuida, Hwa-Kyung Lu, C. M. Fortmann, Isamu Shimizu
Outline: * Background * Two-Step Growth Method * Experimental Results * Interface Structure (Ellipsometry) * Influence of Seed Crystal * Summary
Substrate Seed crystal poly-Si grain Substrate

## Slide 3: SLIDE 2: Background

## Slide 4: Text
Fabrication of Polycrystalline Silicon Thin Films by PE-CVD Method Using SiF4 Source Gas * Highly crystalline poly-Si at low temperatures (200~350C) * High deposition rate (~10Å/s) * High orientation (e.g., (022) growth on glass substrates)
Need to reduce amorphous layer at initial deposition stage * Layer-By-Layer Method * Two-Step Growth Method Background

## Slide 5: SLIDE 3: Two-Step Growth Method

## Slide 6: Text
Two-Step Growth Method Growth Process Substrate Epitaxial-like growth Low-temperature deposition (200~350C) Fast deposition rate poly-Si
Seed Crystal Process Substrate Seed crystal ~100nm High orientation High crystallinity High-temperature deposition Ts (> 360C) Layer-By-Layer Method

## Slide 7: SLIDE 4: Evolution of during Deposition

## Slide 8: Text
0510152002000400060008000 on P-doped poly-Si SiF4 50 sccm SiF4 40 sccm SiF4 30 sccm Time (sec)

## Slide 9: Figure
Figure 1 of Slide 4

## Slide 10
Figure 2 of Slide 4 Figure 3 of Slide 4 Figure 4 of Slide 4 Figure 5 of Slide 4 Figure 6 of Slide 4 Figure 7 of Slide 4 Figure 8 of Slide 4 Figure 9 of Slide 4 Figure 10 of Slide 4 Figure 11 of Slide 4 Figure 12 of Slide 4 Figure 13 of Slide 4 Figure 14 of Slide 4 Figure 15 of Slide 4 Figure 16 of Slide 4

## Slide 11: SLIDE 5: Objective

## Slide 12: Text
Objective 1. Achieve an epitaxial-like interface between the seed crystal and the grown polycrystalline thin film using the two-step growth method. 2. Investigate the influence of the seed crystal’s crystallinity on the properties of the grown polycrystalline thin film.

## Slide 13: SLIDE 6: Experimental Setup

## Slide 14: Text
Experimental Setup Modulator Susceptor MBP Auto Vacuum Controller Ar/H2 SiF4 Shutter in-situ Spectroscopic Ellipsometer Substrate Light source Controlled by Sequencer Layer-By-Layer Method H2 SiF4 Process time Gas flow 0 Deposition Atomic Hydrogen Treatment Crystallinity enhancement Detector Microwave Magnet

## Slide 15: SLIDE 7: Experimental Methods

## Slide 16: Text
Experimental Methods Structural evaluation: Spectroscopic Ellipsometer (SE) X-ray Diffraction (XRD)
Observation of deposition process: Ellipsometry ( at 4.15eV)
Typical deposition conditions

## Slide 17: Figure
Figure 1 of Slide 7

## Slide 18
Figure 2 of Slide 7

## Slide 19: SLIDE 8: Evolution of during the Growth Process

## Slide 20: Text
Evolution of during the Growth Process (SiF4/H2: Same for seed crystal process and growth process) (Seed: 50/5/30, 380C - poly-Si: 50/5/30)

## Slide 21: Figure
Figure 1 of Slide 8

## Slide 22: SLIDE 9: Evolution of during the Growth Process

## Slide 23: Text
Evolution of during the Growth Process (SiF4/H2: Increased SiF4 flow rate in seed crystal process) (Seed: 50/5/60, 380C - poly-Si: 50/5/30)

## Slide 24: Figure
Figure 1 of Slide 9

## Slide 25: SLIDE 10: Evolution of during the Growth Process

## Slide 26: Text
Evolution of during the Growth Process (SiF4/H2: Further increased H2 flow rate in growth process) (Seed: 60/5/60, 380C - poly-Si: 60/10/30)

## Slide 27: Figure
Figure 1 of Slide 10

## Slide 28: SLIDE 11: Influence of Seed Crystal on the Structure of Thin Films Fabricated by the Two-Step Growth Method

## Slide 29: Text
Influence of Seed Crystal on the Structure of Thin Films Fabricated by the Two-Step Growth Method

## Slide 30: Figure
Figure 1 of Slide 11

## Slide 31: SLIDE 12: Seed Crystal Dependence of Evolution during the Growth Process

## Slide 32: Text
Seed Crystal Dependence of Evolution during the Growth Process Seed: 60/5/60 Seed: 60/10/60 (poly-Si: 60/10/60)

## Slide 33: Figure
Figure 1 of Slide 12

## Slide 34
Figure 2 of Slide 12

## Slide 35: SLIDE 13: Influence of Seed Crystal on the Structure of Thin Films Fabricated by the Two-Step Growth Method

## Slide 36: Text
Influence of Seed Crystal on the Structure of Thin Films Fabricated by the Two-Step Growth Method Seed: 60/5/60 Seed: 60/10/60 Diffraction intensity / counts (poly-Si: 60/10/60)

## Slide 37: Figure
Figure 1 of Slide 13

## Slide 38
Figure 2 of Slide 13 Figure 3 of Slide 13 Figure 4 of Slide 13

## Slide 39: SLIDE 14: Summary

## Slide 40: Text
Summary * The interface structure was improved by controlling gas flow rates in both the seed crystal process and the growth process. * The structure of the seed crystal significantly influences the final film structure.