## Slide 1: チュートリアル： 誘電物性
東京科学大学
総合研究院
元素戦略MDX研究センター
フロンティア材料研究所
神谷利夫

## Slide 2
材料の機能とは何か？
Hadis Morkoc and Umit Ozgur, Zinc Oxide, Wiley-VCH
強誘電性 (圧電性)
誘電性 焦電性

## Slide 3: What is dielectrics?
Characterized by electrical conductivity  (typically > 10-8 S/cm)
Electrical conductor (semiconductor, metal)
Characterized by very small electrical conductivity  (typically << 10-8 S/cm)
and by dielectric constant 
Insulator
Dielectrics
Good dielectrics (usually)
are good electrical insulator (very small ) to minimize dielectric loss and leakage current
have high  to storage large charges at low applied voltage
Classified to paraelectics (dielectrics), ferroelectrics, anti-ferroelectrics

## Slide 4: Dielectric permittivity
No electric polarization without external field E
Macroscopic polarization is induced by external field
Uniform P in the bulk region produces the surface charge Q = |P|
E
P
+ + + + + +
– – – – – –
Q = |P|
–Q = –|P|
: Polization density
: Dielectric permittivity (Dielectric constant)
: Dielectric susceptivity

## Slide 5: Dielectric permittivity
Electric susceptibility
Definition of electric flux density D
 : Dielectric constant (permittivity)
: Relative dielectric constant

## Slide 6: Representative dielectric crystals
of representative crystals
CaO 11.8 MgO 9.8
SrO 13.3 KBr 4.78
KCl 4.68 KF 6.05
KI 4.94 LiI 11.03
LiCl 11.05 NaCl 5.62 TiO2 (rutile) //c: 173, in a-b: 89
SnO2 (rutile) //c: 9.9, in a-b: 14
Pb(Zr0.52Ti0.48)O3 (25oC) up to 1600
Mg
O
General trend (there should be many exceptions)
Rock-salt structure (usually < 10)
O
Ti
Rutile structure TiO2 have large ~180
O
Ti
Ba
Perovskite structure Many extraordinary high > 103 (anti-)ferroelectrics, piezoelectrics

## Slide 7: Why perovskite-type crystals exhibit high ?
O
B
A
Aサイトイオン: イオン半径 rA
Bサイトイオン: イオン半径 rB
酸化物イオン: イオン半径 rO
For ideal cubic perovskite structure: Each ion makes just contact with neighbor ions if their ion radii satisfy
For t apart from 1.0, the cubic structure would be distorted:
t | Lattice | Explanation | Example
>1 | Hexagonal | Large rA Small rB | BaNiO3
0.9-1 | Cubic | Ideal contact | SrTiO3, BaTiO3
0.71 - 0.9 | Orthorhombic Rhombohedral | Small rA in B ion interstitial | GdFeO3 (Orth.) CaTiO3 (Orth.)
<0.71 | Different structures | Samll rA, rB | FeTiO3 (Tri.)
Structural instability
by the sub-lattice structure
Case 1:
Unit cell is stabilized by B-O A ion is loosely embedded
Case 2:
Unit cell is stabilized by A-O B ion is loosely embedded
Tolerance factor

## Slide 8: Types of Dielectrics
Paraelectics (dielectrics)
No electric polarization without external field E Spontaneous polarization = 0
Ferroelectrics
Finite polarization exists without external field
Anti-ferroelectrics Local polarizations are ordered in anti-parallel
Macroscopic polarization is induced by external field
Electron cloud ne-
Nuclear (ne+)
E
P
E
Local polarizations are aligned by external field
E
Local polarizations are aligned by by external field
E
Local polarizations are aligned by strong external field
(Ionic) polarization due to asymmetric local structure

## Slide 9
Classification of ferroelectrics related phases
Dielectrics:
Symmetry: any Spontaneous polarization: not necessary
Piezoelectircs: Part of dielectirics, Stress induces surface charges (voltage) / Voltage induces strain
Symmetry: non-centrosymmetric Spontaneous polarization: not necessary (e.g., Wurtzite-type GaAs)
21 Space groups: 1, 2, m, 222, mm2, 4, -4, 422, 4mm, -42m, 3, 32, 3m, 6, -6, 622, 6mm, -62m, 23, -43m, 432
Pyroelectircs: Part of piezoelectrics, Temperature change induces spontaneous polarization change and surface charge change
Symmetry: non-centrosymmetric & polar Spontaneous polarization: necessary
10 Space groups: 1, 2, m, mm2, 4, 4mm, 3, 3m, 6, 6mm
Ferroelectrics: Part of pyroelectrics, polarization is flipped by external electric field
Symmetry: non-centrosymmetric & polar Spontaneous polarization: necessary
10 Space groups: 1, 2, m, mm2, 4, 4mm, 3, 3m, 6, 6mm
Dielectrics
piezoelectrics
pyroelectrics
ferroelectrics

## Slide 10
誘電体の応用

## Slide 11: 1. 強誘電体メモリー (FeRAM) 1999: 富士通のFeRAM混載LSI 2006: ソニーの FeliCaに採用 2. 抵抗変化メモリー (ReRAM) 2013: パナソニック 8bit ｺﾝﾋﾟｭｰﾀ (Ta2O5) サンプル出荷 3. エレクトロクロミック 一部の自動車用防眩ルームミラー 4. 圧電セラミックス 加速度センサー、圧電ジャイロ 5. ディスプレイ用薄膜トランジスタ 2012~: スマートフォン, 80” LCD, 88” OLED TV
実用化された酸化物機能材料

## Slide 12: Application of dielectrics: Capacitor
Capacitor: Storage charges by applied voltage V
+ + + + +
– – – – –
VC
+QC
–QC
: Relative dielectric constant
S : Electrode area of the capacitor
d : Electrode distance
Circuits: Low (High) pass filter Oscillator Combined with resistor, inductor

## Slide 13: Application of dielectrics: DRAM
“1”
“0”
Capacitor: (memory node)
Tr: Transistor (switch)
Vsw
VC
Leak current through transistor and capacitor, Ioff
Retention time
=
DRAM (dynamic random access memory)
+ + + + +
– – – – –
VC when Tr is on

## Slide 14: Application of dielectrics: FET
Two representative functions of transistor 1. Amplification Use linear region (IDS  VGS) 2. Switching Use large on/off current ratio
VGS
IDS
Leak current: power consumption
Off state
On current
On state
At VGS = 0V On state: Normally-on Depletion-type Off state: Normally-off Enhancement-type
dielectrics
Drain VDS
gate VGS
source
carrier
IDS
semiconductor
FET (Field-effect transistor)

## Slide 15: 強誘電体の応用例
Ferroelectric gate
Drain VDS
gate VGS
source
IDS
semiconductor
FeRAM (強誘電体メモリ)
Memory state “0”
N-type semi.
–Ps induces positive charge at the insulator-semiconductor interface, but n-type semi does not induce mobile carriers
=> FET is “Off” state
–Ps
Gate dielectric in conventional FET is replaced with ferroelectrics
Spontaneous polarization Ps retains if gate voltage VGS is off
=> 不揮発メモリ
Memory state “1”
N-type semi.
+Ps induces negative charge at the insulator-semiconductor interface, so n-type semi induces mobile celectron arriers
=> FET is “On” state
+Ps

## Slide 16: 圧電体の応用例
Scanning Probe Microscope (SPM)
Atomic Force Microscope (AFM)
Scanning Tunneling Microscope (STM)
Wikipedia: https://ja.wikipedia.org/wiki/%E8%B5%B0%E6%9F%BB%E5%9E%8B%E3%83%88%E3%83%B3%E3%83%8D%E3%83%AB%E9%A1%95%E5%BE%AE%E9%8F%A1
piezoelectrics is used as piezoactuator
Fast response, atomic-order precision
PZT: d33 = 400x10-12 m/V
33 = l / l = d33E
For V = 100 V, l = 1 cm,
33 = d33E = 400x10-8
l = 400 Å
For V = 0.1 V
l = 0.4 Å

## Slide 17: 圧電体の応用例
Surface Acoustic Wave (SAW) filter
Surface acoustic wave is induced by piezoelectrics
SAW is resonant with the piezoelectric body at the frequency fr => Transmit signals with f ~ fr: Band pass filter
fr: up to several GHz, used e.g. in mobile phones
https://www.murata.com/ja-jp/group/kanazawamurata/products/device/saw
SAW
In-plane comb electrodes
piezoelectric substrate
signal
signal

## Slide 18: Electromagnetism equations
Gauss law
Ampere-Maxwell law
Non-existence of magnetic monopole
Electromagnetic induction law
Electric field and electrostatic potential
Poisson equation
Charge conservation law
Maxwell equation
Derivatives

## Slide 19: Electromagnetism equations
Ohm’s law (Electrical conductivity)
Electric susceptibility
Constitutive equations (material equations)
Dielectric permittivity (Dielectric constant)
Relative dielectric permittivity (constant)
Magnetic susceptibility
Magnetic permeability

## Slide 20: Electric polarization
Definition of electric polarization p
-q
+q
r = r+ – r-
r-
r+
Two point charges +q and –q are located at r+ and r-, respectively.
General definition of electric polarization density, P
N point charges with qi are located at ri, respectively, in the volume V.
Note: Uniquely defined only when the charge neutrality is satisfied.

## Slide 21
反電場

## Slide 22
Internal macroscopic field is different from external field: Depolarization field
External field E0: formed by the charges on the electrodes Qe
Surface charges: induced from internal polarization
, which forms extra electric field:
Internal macroscopic field in the dielectrics:
General shapes of dielectrics: E1,s = , Ns: Depolarization factors (s = x, y, z)
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 457
+ + + +
+ + +
–
–
–
–
–
–
–
E0
P
–QP
+QP
E = E0 + E1
+Qe
–Qe
E1

## Slide 23
is defined by internal electric field E :
=>
Internal macroscopic field is different from external field: Depolarization field
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 457
+ + + +
+ + +
–
–
–
–
–
–
–
E0
P
–QP
+QP
E = E0 + E1
+Qe
–Qe
E1

## Slide 24
Macroscopic theory => Microscopic theory
Understand properties of dielectric from those of atoms/ions
Polarizability of the atom i () is defined by atomic polarization and local electric field
How is different from the macroscopic internal field E ?

## Slide 25
E0
Internal electric field at an atomic site: Lorentz field
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 460
At an atom site r0, polarizations from surrounding atoms form an extra field: Lorentz field R2: Contribution to Elocal at r0, the center of the sphere, is calculated by summing up the ion charges in R2. => the net charges appear on the surface of the sphere
: Lorentz field
For cubic symmetry
+ + + +
+ + +
–
–
–
–
–
–
–
-QP
+QP
E1
R1
R2
–
–
–
+
+
+
-qP
+qP
E2
Elocal
E = E0 + E1
+Qe
–Qe

## Slide 26
Atom polarizability to dielectric permitivity
Polarizability of the atom i () is defined by atomic polarization and
Assume the atomic polarization is independent from each other.
Using
Clausius-Mossotti relation

## Slide 27
Effect of local field correction
Without local field correction
With local field correction
Chart: 
| 0 | 0.2 | 0.4 | 0.6 | 0.8 | 1 | 1.2 | 1.4 | 1.6 | 1.8 | 2 | 2.2000000000000002 | 2.4 | 2.6 | 2.8 | 3
w/o local field correction | 1 | 1.2 | 1.4 | 1.6 | 1.8 | 2 | 2.2 | 2.4 | 2.6 | 2.8 | 3 | 3.2 | 3.4 | 3.6 | 3.8 | 4
local effect correction | 1 | 1.2143 | 1.4615 | 1.75 | 2.0909 | 2.5 | 3 | 3.625 | 4.4286 | 5.5 | 7 | 9.25 | 13 | 20.5 | 43

## Slide 28
Simple model of electronic polarizability
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 464

## Slide 29
Electronic polarizability
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 464
Total polarizability may be separated into (i) electronic, (ii) ionic, and (iii) dipolar / interfacial parts.
Drude-type relaxation
Ionic
(phonon)
electronic
dipolar interfacial
Lorentz-type
(resonant-type) relaxation

## Slide 30
Frequency dependence: Lorentz model
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 466
Similar expression is obtained by quantum theory
ij: Transition energy from I to j states fij : Oscillator strength
Generalized to ion displacement polarization
Shell model: Electron bound by spring constant k
nuclei
electron
x
Elocal
Classical mechanics approximation
Electronic polarizability
Frequency dependence:

## Slide 31
Frequency dependence: Drude model
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 466
nuclei
electron
x
Elocal
Classical mechanics approximation
Electronic polarizability

## Slide 32: Lorentz model and Drude model
Lorentz model is derived from :
The recovery force results in the resonant-type relaxation with the relaxation frequency.
: Applied to electronic polarization in atom, ionic polarization (phonon)
For the case of no recovery term: Drude model with scattering
For : , ,
: Plasma frequency
Notes: 32

## Slide 33
縦光学 (LO) フォノンが作る反分極場
-q
+q
: 付加的な復元力 => 振動数を上げる
縦光学 (LO) フォノン
横光学 (TO) フォノン
無分極状態
k
フォノン分極による
局所場は発生しない
Non-analytical term
変位
変位
x
z
k
局所場

## Slide 34
TOフォノンとLOフォノンの寄与: LSTの式
フォノンが形成した分極が空間的に均一であれば、
Maxwellの方程式より
の時、
LOフォノンでは であるから、
TOフォノンでは であるから、
Clausius-Mossotiの式を 1周波数の場合に簡単化する
=>
の条件から
: Lyddane-Sachs-Teller (LST) の式

## Slide 35: Lyddane–Sachs–Teller relation
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 414
中村輝太郎 編著、強誘電体構造相転移 (裳華房, 1988)
Lyddane–Sachs–Teller–Kurosawa (LSTK) relation
Lyddane–Sachs–Teller (LST) relation
: Resonance frequency of transversal phonon Polarization formed by phonon is macroscopically zero.
: Resonance frequency of longitudinal phonon Polarization formed by phonon gives recovery force to phonon: Higher than
Possible to estimate from infrared / Raman spectrum
At : = 0
At : = 0
Notes: 35

## Slide 36
縦／横光学フォノン

## Slide 37: Lyddane–Sachs–Teller relation
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 414
中村輝太郎 編著、強誘電体構造相転移 (裳華房, 1988)
Lyddane–Sachs–Teller–Kurosawa (LSTK) relation
Lyddane–Sachs–Teller (LST) relation
: Resonance frequency of transversal phonon Polarization formed by phonon is macroscopically zero.
: Resonance frequency of longitudinal phonon Polarization formed by phonon gives recovery force to phonon: Higher than
Possible to estimate from infrared / Raman spectrum
At : = 0
At : = 0
Notes: 37

## Slide 38
縦光学 (LO) フォノン振動数はBZ境界で不連続になる
+
+
+
+
ー
ー
ー
ー
ー
k
kがx方向 kx
変位 : LOフォノン
k
kがz方向に変わると kz
変位 : TOフォノン
LOフォノン
LOフォノンだったが、
TOフォノンに変化
同じ基準モードの
TOフォノン
kx kz
フォノン振動数
Γ
X
Z

## Slide 39
構造不安定性と強誘電性

## Slide 40
4/3 catastrophe: Slater theory of ferroelectricity
With local field correction
Diverges at
=> Spontaneous polarization
Slater‘s 4π/3 instability (in CGS unit)
If : Curie-Weiss law
Chart: 
| 0 | 0.2 | 0.4 | 0.6 | 0.8 | 1 | 1.2 | 1.4 | 1.6 | 1.8 | 2 | 2.2000000000000002 | 2.4 | 2.6 | 2.8 | 3
w/o local field correction | 1 | 1.2 | 1.4 | 1.6 | 1.8 | 2 | 2.2 | 2.4 | 2.6 | 2.8 | 3 | 3.2 | 3.4 | 3.6 | 3.8 | 4
local effect correction | 1 | 1.2143 | 1.4615 | 1.75 | 2.0909 | 2.5 | 3 | 3.625 | 4.4286 | 5.5 | 7 | 9.25 | 13 | 20.5 | 43
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 471
中村輝太郎 編著、強誘電体と構造相転移 (裳華房、1988)

## Slide 41
Ferroelectrics
Temperature dependences for PbTiO3
diverges and discontinuously changes at the transition temperature
(Curie temperature) TC, like :
transition
Feature of first order phase transition
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 467
TC
T > TC
Cubic structure
No spontaneous polarization
T < TC stabilizes
ions displaced and
lattice distorted => Spontaneous polarization

## Slide 42
Spontaneous polarization and double-well potential
疋田朋幸 訳 (B.A. Strykob, A.P. Rebaniok)、強誘電体物理入門 (吉岡書店, 1993)
P
+E
P
–E
Ps : Spontaneous polarization
Ecor: Coercive electric field
Ps
P
E
Ecor

## Slide 43
Equilibrium polarization is obtained by
To explain ferroelectric transition (Curie-Weiss law),
Landau Theory of Phase Transition
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 474
Perovskite-type ferroelectrics takes cubic crystal structure in the paraelectric phase (high temperature) => Free energy is expanded by

## Slide 44
Landau Theory of Phase Transition
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 476
Consider E = 0 for spontaneous polarization
Second-order transition
If g4 is positive, the g6 term has no effect and can be neglected.
For :
For :
LiTaO3

## Slide 45
Landau Theory of Phase Transition
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 477
First-order transition
If g4 is negative, the g6 term must be retained.
or
Ps discontinuously changed to zero
温度の上昇とともに 原点でのポテンシャル曲率が負から正へ

## Slide 46
ソフトモード理論
温度の上昇とともに 原点でのポテンシャル曲率が負から正へ
温度の低下とともに
・ ある 光学フォノン周波数が 0 に近づく
・ 原子の変位は大きくなる
高温の高対称相から見ると
温度 TC で
・ 光学フォノンの振動数が 0 になる
・ 原子の変位が凍結される
ソフトモード
Γ点ソフトモード: 強誘電転移
X点ソフトモード: <100>反強誘電転移 R点ソフトモード: <111>反強誘電転移

## Slide 47
大きな誘電率を持つ物質とTOフォノン、相転移
・ イオンを束縛しているポテンシャルが緩やか
ポテンシャルの曲率 ∝ ωTO2
ωTO周波数が低い  LSTの関係)
・ 温度、圧力で ωTO が減少: ソフトモード
・ 構造不安定性を誘起: ωTO2 < 0 (虚数モード)
ソフトモードがΓ点 : 強誘電体転移
ソフトモードがBZ境界: 反強誘電体転移

## Slide 48
Ferroelectricity and Anti-ferroelectricity
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 478
P
P
P
P
P
P
P
P
P
P
pyroelectric
Γ point: ferroelectric
X point: antiferroelectric
T > TC
T < TC
T < TC
Apply large reverse field
Finite Ps
Ps not necessary reversed by E
Finite Ps
Ps must be reversed by E
Finite local Ps , macroscopic Ps is cancelled Local Ps can be reversed by large E and may exhibit ferroelectric behavior

## Slide 49
Sequential phase transition of BaTiO3
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 471
三井利夫 編著、強誘電体 (槇書店, 1969)
BaTiO3の逐次相転移:
立方晶、常誘電体
正方晶、強誘電体 <100>ソフトモードの凍結
直方晶、強誘電体 <110>ソフトモードの凍結
菱面晶、強誘電体 <111>ソフトモードの凍結

## Slide 50
Ferroelectrics: BaTiO3
ｒ
T (oC)
a
c
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 471
三井利夫 編著、強誘電体 (槇書店, 1969)

## Slide 51
Anti-ferroelectricity
Kittel, Introduction to Solid State Physics, 8th ed (2005) p. 479
Ferroelectic (tetragonal)
PZT: PbTiO3 – PbZrO3
PbTiO3: Ferroelctrics
PbZrO3: Antiferroelectrics
Ferroelectic (rhombohedral 1)
Anti-ferro
Ferro (rhomb 2)
MPB
(Morphotoropic phase bounary)

## Slide 52
Two types of ferroelectricity
Displacement type ferroelectric
Small displacement of ions form Ps
(Ions are bound by recovery force to the high-symmetric position)
Order-disorder type ferroelectric
Perovskite type crystals
BaTiO3, Pb(Zr,Ti)O3
Ions find different stable positions in high-symmetry structure, hop to another site in a long distance
NaNO2 : NO2 group KDP (KH2PO4): H+
強誘電体物理入門