Defect statistics:

- Definitions

Crystal has crystallographic sites S, and S can be a defect substituted with an atom/vacancy A with the charge state q, ASq. For example, in ZnO, {S} = {Zn, O, i1, i2}, {A} = {O, Zn, Ga, V}, {q} = {-2, -1, 0, +1, +2}, then the defects can be GaZn+, GaZn0, VO2+, VO+, VO0 etc.

As derived in Section 1, canonical statics is applied to each site, that is, the defect densities are

nS,A,q(T)=NSexp-ES,A,q/kT/ZS,totT 					(1-10)

, where NS is the density (number) of the S site, ES,A,qis the formation energy of ASq with respect to the energy of the ideal crystal, and ZS,totT=1+ZS(T) is the partition function for the site S.

ZS,totT=1+ZST=1+A,qexp-ES,A,q/kT 				(1-11)

, where the first term of the right-hand equation corresponds to exp-ES,A,q/kT=1 of the ideal site (ES,A,q=0).

Here we define partial partition functions, which do not include the ideal site case,

ZST=A,qexp-ES,A,q/kT 						(i-1)

ZS,AT=qexp-ES,A,q/kT 						(i-2)

From eq. (1-10), the total density of the AS defects is given by

nS,A(T)=NSqexp-ES,A,q/kT/1+ZS(T)=NSZS,AT/1+ZS(T) 	(i-3)

, and the total density of the defects for site S is

nS(T)=NSA,qexp-ES,A,q/kT/1+ZS(T)=NSZST/1+ZS(T) 		(i-4)

Then, the density of the ideal sites for site S is

nS,ideal(T)=NS1-ZST/1+ZS(T)=NS/1+ZS(T) 			(i-5)

- Defects frozen at Tdef

The total defect density at site S is

nS(Tdef)=NSZSTdef/1+ZS(Tdef) 					(ii-1)

nS,A(Tdef)=NSZS,ATdef/1+ZS(Tdef) 					(ii-2)

- Charge states at T for the defects frozen at Tdef: Perfect freeze case

Upon the condition the defects created at Tdef in (ii) are maintained and no extra defects are created at lower temperatures, T, the q charge states of the defect AS are given by

nS,A,qT=nS,ATdefexp-ES,A,qkT/ZS,AT

=NSZS,ATdef/1+ZS(Tdef)×exp-ES,A,q/kT/ZS,A(T) 		(iii-1)

Note that the partition function in (iii-1) does not include the ideal site as this site S is supposed to be a defect, so the partition function is the partial partition function ZS,AT.

- Check the case Tdef = T

From eq. (iii-1),

nS,A,qT=NSexp-ES,A,q/kT/1+ZS(T) 					(iv-1)

is obtained, being consistent with eq. (1-10).

======================================================================================

- Statistics at given T

Defects at a S site can take different states like: SS0 (no defect), VS2-, VS-, VS0, VS+, VS2+, GaS2+ etc, which are expressed by

{i} = {ASq} (i = 1,2,⋯NS,NLS)				(1-1)

. Therefore following constraints should be applied in the scheme of canonical ensemble. i.e.,

The total site number:

NS=inS,i 						(1-2)

, where nS,i denote the number of the sites with the i state,

For the entire system, the total energy should be

E=S,iES,inS,i 						(1-3)

, where ES,i denote the formation energy of the site with the i state.

The total configuration numbers is expressed as

W=W0SWS 						(1-4)

, where W0=1 is the configuration number of the ideal sites, and WSdenote the configuration numbers of the site S.

WS=NS!nS,1!nS,1!⋯nS,NLS! 					(1-5)

. To obtain maximally probable configuration, the following function F should be maximized with the constraint parameters of the Lagrange’s multiplier method (for eqs. (2) and (3)),

F=lnW+SαSinS,i-NS+βS,iES,inS,i-E 		(1-6)

Using the Stirling’s approximation

lnNS,i!~nS,ilnnS,i-nS,i 					(1-7)

eq. (6) will be approximated by

F~NSlnNS-NS-inS,ilnnS,i-nS,i+SαSinS,i-NS+βS,iES,inS,i-E		(1-6’)

To minimize F with respect to nS,i,

∂F∂nS,i=-lnnS,i+αS+βES,i=0				(1-8)

Then

nS,i=expβES,i+αS 					(1-9)

As explained in textbooks of statistical physics,

β=-1kT

and expαS is determined by eq. (2). Then,

nS,i(T)=NSexp-ES,i/kT/ZS(T) 					(1-10)

, where ZS is the partition function for the site S.

ZS(T)=i in Sexp-ES,i/kT 					(1-11)

This result means that we should apply the canonical statistics to each site independently.

Note that i includes the ideal model, which ES,i is normalized to 0 and ZS is approximated to ~1 if all ES,i satisfy

ES,ikT≫1 							(1-12)

Then usual expression

nS,i(T)~NSexp-ES,i/kT 					(1-13)

is obtained.

Ignore below =============================================================================

- Defect densities at Tdef

Given by

nS,iTdef=NSexp-ES,i/kTdef/ZSTdef 					(2-1)

ZSTdef=i in Sexp-ES,i/kTdef 					(2-2)

, giving the total defect densities at the site S:

nSTdef=i' is not ideal statenS,i'Tdef 					(2-3)

- Charged states of defects at T for the defect densities frozen at Tdef: Consider only the frozen defects

We here consider only nS,iTdef remain and are formed at T lower than Tdef. The atomic defect structures are frozen and therefore those can take different charge states only, where the ideal state must be exclude. I.e., the defect states are expressed only by the charge states q..

{q} = {-2, -1, 0, +1, +2 etc}								(3-1)

Then, we obtain

nS,q(q)T=nSTdefexp-ES,q/kT/ZS(q)T

=NSi' is not ideal stateexp-ES,i'/kTdef/ZSTdef×exp-ES,q/kT/ZS(q)	(3-2)

ZS(q)T=qexp-ES,q/kT							(3-3)

Note that ZS(q)T does not include the ideal state and cannot be approximated to 1.

If one ES,q (q = q’) is satisfactory smaller than the other ES,q, ZS(q)T~exp-ES,q/kT and

nS,q'(q)T~nSTdef								(4-2)

This result would be consistent with our intuitive conclusion, where all the defects take the lowest energy state.

- What happens if T = Tdef

In principle, eq. (3-2) must be identical to eq. (1-10) if T = Tdef.

nS,i(T)=NSexp-ES,i/kT/ZS(T) 							(1-10)

ZS(T)=i in Sexp-ES,i/kT 							(1-11)

nS,qqT=nSTexp-ES,q/kT/ZS(q)T

=NSi' is not ideal stateexp-ES,i'/kT/ZST×exp-ES,q/kT/ZS(q)(T)

=nS,i(T)i is not ideal stateexp-ES,i'/kT/ZS(q)				(3-2’)

ZS(q)T=qexp-ES,q/kT							(3-3’)

nS,qqT/nS,q(T)=nST/ZS(q)T×ZS(T)/NS  					(4-1)

- Charged states of defect at T for the defect densities frozen at Tdef: More realistic case. Additional formation of thermal equilibrium defects at T

We need to consider nS,iTdef and NS-nS,iTdef separately for the site S because the former sites cannot change structure and can change charged state only, while the latter can produce/change defect states by thermal equilibrium. Therefore, former counts only different charge states and must exclude the ideal state.

{q} = {-2, -1, 0, +1, +2 etc}							(16)

and

nS,i(1)T=nS,iTdefexp-ES,i/kT/ZS(1)T

=NSexp-ES,i/kTdefexp-ES,i/kT/ZS(1)/ZSTdef		(17)

ZS(1)T=qexp-ES,q/kT						(18)

Note that ZS(1)T does not include the ideal state and can not be approximated to 1.

Whil

- Charged states of defect at T for the defect densities frozen at Tdef

We need to consider nS,iTdef and NS-nS,iTdef separately for the site S because the former sites cannot change structure and can change charged state only, while the latter can produce/change defect states by thermal equilibrium. Therefore, former counts only different charge states and must exclude the ideal state.

{q} = {-2, -1, 0, +1, +2 etc}							(16)

and

nS,i(1)T=nS,iTdefexp-ES,i/kT/ZS(1)T

=NSexp-ES,i/kTdefexp-ES,i/kT/ZS(1)/ZSTdef		(17)

ZS(1)T=qexp-ES,q/kT						(18)

Note that ZS(1)T does not include the ideal state and can not be approximated to 1.

while the latter follows the discussion in Section 1.

nS,i(2)T=NS-nS,iTdefexp-ES,i/kT/ZST 				(18)

ZST=iexp-ES,q/kT 						(19)

Then total defect states at T for the defects frozen at Tdef are given by

nS,iT=NSexp-ES,i/kTdefexp-ES,i/kT/ZS(1)/ZSTdef

+NS-nS,iTdefexp-ES,i/kT/ZST 				(20)

- Consistency check.

One requirement for eq. (20) is that the case Tdef = T must be equal to eq. (10).

nS,i'T=nS,iTexp-ES,i/kT/ZS(1)T +NS-nS,iTexp-ES,i/kT/ZST

=nS,iT+nS,iTexp-ES,i/kT1ZS1T-1ZST

~nS,iT+nS,iTexp-ES,i/kT/ZS1T 			  	(21)

for i is not the ideal state.

This condition is satisfied only if nS,iT≪NS i.e.,ES,ikT≫1.