## Slide 1: Band filling correction: Correction to dilution limit
Small super cell (high defect dens.)
Infinite cell (dilute. limit)
Log (DOS)
CB
VB
EF
e- energy
E0,dil
Log (DOS)
CB
VB
e- energy
EF ~ E0,dil
Extra energy
for donor case
Summation is taken over the electrons having extra energy in CB / defect states
Walle and Neugebauer, J. Appl. Phys. 9 (2004) 3851; Oba et al., Sci. Technol. Adv. Mater. 12 (2011) 034302
Notes: 1

## Slide 2: Band filling correction: Hole / acceptor case
Small super cell (high defect dens.)
Infinite cell (dilute limit)
Log (DOS)
CB
VB
EF
e- energy
E0,dil
Log (DOS)
CB
VB
e- energy
EF ~ E0,dil
Extra energy
for acceptor case
Summation is taken over the electrons having extra energy in VB / defect states
Notes: 2

## Slide 3
Configuration on TSUBAME
Directories:
$DataRoot/bin/Databases DB files required for python/perl scripts
$DataRoot/bin/python
$DataRoot/bin/python/lib python modules, should be in PYTHONPATH
$DataRoot/bin/python/vasp python vasp scripts
$DataRoot/bin/Perl
$DataRoot/bin/Perl/lib perl modules, should be in PERL5PATH
$DataRoot/bin/Perl/VASP perl vasp scripts
Aliases:
alias vasp_input="python $PythonVASPDir/vasp_input.py"
alias vasp_plot_band="python $PythonVASPDir/vasp_plot_band.py"
alias vasp_plot_dos="python $PythonVASPDir/vasp_plot_dos.py"
alias vasp_plot_epsilon="python $PythonVASPDir/vasp_plot_epsilon.py"
alias vasp_output="python $PythonVASPDir/vasp_output.py"
alias vasp_md_history="python $PythonVASPDir/make_md_history.py"
alias vasp_outcar2axsf="python $PythonVASPDir/outcar2axsf.py"
alias vasp_correction_bandfilling="python $PythonVASPDir/vasp_correction_bandfilling.py"
alias vasp_correction_VBM="python $PythonVASPDir/vasp_correction_VBM.py"
alias vasp_correction_charge="python $PythonVASPDir/vasp_correction_charge.py"
alias vasp_defect="python $PythonVASPDir/vasp_defect.py"

## Slide 4
Example data directory structure
TSUBAME: Data root: $DataRoot/Data-kamiya/Defect
Working dir: copy Defect to your home Windows:
Data root: vasp/Defect
Working dir: vasp
Ideal model: ./Defect/ZnO VCRelax: Full relaxation with high accuracy SCF : SCF DOS : DOS BandX : Band structure
VO model (neutral): ./Defect/ZnO-VO VCRelax: Fixed-cell relaxation with high accuracy SCF : SCF
VO model (+1e charged): ./Defect/ZnO-VOp1 VCRelax: Fixed-cell relaxation with high accuracy SCF : SCF

## Slide 5
Band structure: Ideal
vasp_plot_band-test.bat
(left) python vasp_plot_band.py band .\Defect\ZnO\BandX
(right) python vasp_plot_band.py bandocc .\Defect\ZnO\BandX
Occupancy is expressed by grey level in the circles

## Slide 6
Density of states: Ideal
vasp_plot_dos-test.bat
python vasp_plot_dos.py DOS .\Defect\\ZnO\DOS

## Slide 7
Optical dielectric function: Ideal
vasp_plot_epsilon-test.bat
python vasp_plot_epsilon.py density eps_i6_hse_LOPT

## Slide 8
EVBM correction: VO0
vasp_correction_VBM-test.bat 0.05
python vasp_correction_VBM.py exclude .\Defect\ZnO\SCF .\Defect\ZnO-VO\SCF
Use mode = Exclude
Output:
Average core potentials:
.\Defect\ZnO\SCF
0000 Zn ( 0.3333, 0.6667, 0.0005) -36.137 eV
0001 Zn ( 0.6667, 0.3333, 0.5005) -36.137 eV
0002 O ( 0.3333, 0.6667, 0.3821) -73.3886 eV
0003 O ( 0.6667, 0.3333, 0.8821) -73.3886 eV
.\Defect\ZnO-VO\SCF
Origin: ( 0.1667, 0.3333, 0.1910)
Zn 0000 (Zn 0000) ( 0.1667, 0.3333, 0.0316) -36.5935 eV - -36.1370 eV = -0.4565 eV (0) 1.656 A
Zn 0001 (Zn 0000) ( 0.1658, 0.8329, 0.0008) -35.8960 eV - -36.1370 eV = 0.2410 eV (1) 3.798 A
Zn 0002 (Zn 0000) ( 0.6671, 0.3342, 0.0008) -35.8960 eV - -36.1370 eV = 0.2410 eV (1) 3.798 A
Zn 0003 (Zn 0000) ( 0.6671, 0.8329, 0.0008) -35.8960 eV - -36.1370 eV = 0.2410 eV (1) 5.95 A
Zn 0004 (Zn 0001) ( 0.3197, 0.1803, 0.2418) -36.5342 eV - -36.1370 eV = -0.3972 eV (0) 1.798 A
Zn 0005 (Zn 0001) ( 0.3197, 0.6394, 0.2418) -36.5344 eV - -36.1370 eV = -0.3974 eV (0) 1.798 A
Zn 0006 (Zn 0001) ( 0.8606, 0.1803, 0.2418) -36.5344 eV - -36.1370 eV = -0.3974 eV (0) 1.798 A
Zn 0007 (Zn 0001) ( 0.8333, 0.6667, 0.2509) -35.8794 eV - -36.1370 eV = 0.2576 eV (1) 3.796 A
Zn 0008 (Zn 0000) ( 0.1667, 0.3333, 0.5011) -35.8566 eV - -36.1370 eV = 0.2804 eV (0) 3.222 A
(cut here)
VBM correction:
dEVBM: 0.220619 eV

## Slide 9
EVBM correction: VO0
vasp_correction_VBM-test.bat 0.05
python vasp_correction_VBM.py mode .\Defect\ZnO\SCF .\Defect\ZnO-VO\SCF
Use mode = mode (mode value, most frequent E)
Output:
Defect sites:
V: O 0000 ( 0.1667, 0.3333, 0.1910)
range: 0.6000000000000001 30
Vcore difference threshold (dVth): 0.1000 eV
Most frequent dVcore (dVmf): 0.2235 eV
Averaged dVcore in dVth (dVav): 0.2206 eV
(cut)
Origin: ( 0.1667, 0.3333, 0.1910)
Zn 0000 (Zn 0000) ( 0.1667, 0.3333, 0.0316) -36.5935 eV - -36.1370 eV = -0.4565 eV (0) 1.656 A
Zn 0001 (Zn 0000) ( 0.1658, 0.8329, 0.0008) -35.8960 eV - -36.1370 eV = 0.2410 eV (1) 3.798 A
Zn 0002 (Zn 0000) ( 0.6671, 0.3342, 0.0008) -35.8960 eV - -36.1370 eV = 0.2410 eV (1) 3.798 A
Zn 0003 (Zn 0000) ( 0.6671, 0.8329, 0.0008) -35.8960 eV - -36.1370 eV = 0.2410 eV (1) 5.95 A
Zn 0004 (Zn 0001) ( 0.3197, 0.1803, 0.2418) -36.5342 eV - -36.1370 eV = -0.3972 eV (0) 1.798 A
Zn 0005 (Zn 0001) ( 0.3197, 0.6394, 0.2418) -36.5344 eV - -36.1370 eV = -0.3974 eV (0) 1.798 A
Zn 0006 (Zn 0001) ( 0.8606, 0.1803, 0.2418) -36.5344 eV - -36.1370 eV = -0.3974 eV (0) 1.798 A
Zn 0007 (Zn 0001) ( 0.8333, 0.6667, 0.2509) -35.8794 eV - -36.1370 eV = 0.2576 eV (1) 3.796 A
Zn 0008 (Zn 0000) ( 0.1667, 0.3333, 0.5011) -35.8566 eV - -36.1370 eV = 0.2804 eV (0) 3.222 A
(cut here)
VBM correction:
dEVBM: 0.220619 eV

## Slide 10
EVBM correction: VO+
vasp_correction_VBM-test.bat
python vasp_correction_VBM.py mode .\Defect\ZnO\SCF .\Defect\ZnO-VOp1\SCF
Output:
Defect sites:
V: O 0000 ( 0.1667, 0.3333, 0.1910)
Vcore difference threshold (dVth): 0.1000 eV
Most frequent dVcore (dVmf): 0.3457 eV
Averaged dVcore in dVth (dVav): 0.3388 eV
(cut) VBM correction:
dEVBM: 0.338824 eV

## Slide 11
Band filling correction: VO0
vasp_correction_bandfilling-test.bat python vasp_correction_bandfilling.py BF .\Defect\ZnO-VO\SCF Adjust EF0 so as to find appropriate EV and EC Default EF0 is 0.1 eV, which seems to be ok Output:
Total weight: 1.0
Total Ne : 141.0
NELECT : 282.0
Count spin degeneration of 2:
Total Ne : 282.0
dEh = 0 eV
dEe = 0 eV
Count spin degeneration of 2:
dEh = 0 eV
dEe = 0 eV

## Slide 12
Band filling correction: VO+
vasp_correction_bandfilling-test.bat python vasp_correction_bandfilling.py BF .\Defect\ZnO-VOp1\SCF
Adjust EF0 so as to find appropriate EV and EC Default EF0 is 0.1 eV, which seems to be ok Output:
Total weight: 1.0
Total Ne : 140.50000003125
NELECT : 281.0
Count spin degeneration of 2:
Total Ne : 281.0000000625
dEh = 0.00235026 eV
dEe = 0.000292896 eV
dEtot = 0.00264315 eV
Count spin degeneration of 2:
dEh = 0.00470051 eV
dEe = 0.000585792 eV
dEtot = 0.00528631 eV

## Slide 13
Band filling correction: Note for VO0
Occupancy in VASP is not at 0 K, and some electrons occupy excited states. In the PBE VO0 case trace electrons exists in CB.
EHOMO is defined as the highest level occupied by electrons greater than 0.0.
Output:
Band filling energy correction:
Band edge from EIGENVAL:
EF0 = 0.100000 eV
EF = 1.723700 => 0.0 eV
EV = -0.200448 eV
EC = 0.146521 eV
Eg = 0.346969 eV
EHOMO = 0.181438 eV
ELUMO = 1.066398 eV
k[ 0]: ( 0.0000 0.0000 0.0000) w= 0.03125
k[ 1]: ( 0.2500 0.0000 0.0000) w= 0.1875
dEh: up iE=140 E= -0.354216 eV dNh= -0.08152 dEh= 0.00235026 eV
k[ 2]: ( 0.5000 0.0000 0.0000) w= 0.09375
dEe: up iE=140 E= 0.181438 eV dNe= 0.04228 dEe= 0.000138396 eV
k[ 3]: ( 0.2500 0.2500 0.0000) w= 0.1875
dEe: up iE=140 E= 0.149776 eV dNe= 0.1239 dEe= 0.000213995 eV
k[ 4]: ( 0.0000 0.0000 0.5000) w= 0.03125
k[ 5]: ( 0.2500 0.0000 0.5000) w= 0.1875
dEh: up iE=140 E= -0.200448 eV dNh= 0.04648 dEh= 0.00235026 eV
k[ 6]: ( 0.5000 0.0000 0.5000) w= 0.09375
dEe: up iE=140 E= 0.160428 eV dNe= 0.06052 dEe= 0.000292896 eV
k[ 7]: ( 0.2500 0.2500 0.5000) w= 0.1875
dEe: up iE=140 E= 0.146521 eV dNe= 0.123 dEe= 0.000292896 eV

## Slide 14
Band filling correction: GaZn0
vasp_correction_bandfilling-test.bat python vasp_correction_bandfilling.py BF .\Defect\ZnO-GaZn\SCF
Adjust EF0 so as to find appropriate EV and EC Default EF0 is 0.1 eV, but the estimated EV seems in CB
CBM
VBM
EF0 should be between CBM and VBM Try EF0 = -2.2 eV (next page)

## Slide 15
Band filling correction: GaZn0
vasp_correction_bandfilling-test.bat python vasp_correction_bandfilling.py BF .\Defect\ZnO-GaZn\SCF
Adjust EF0 so as to find appropriate EV and EC Default EF0 is 0.1 eV, but the estimated EV seems in CB Try EF0 = -2.2 eV vasp_correction_bandfilling-test.bat -2.2 Output:
Total weight: 1.0
Total Ne : 139.49999999999997
NELECT : 279.0
Count spin degeneration of 2:
Total Ne : 278.99999999999994
dEh = 0 eV
dEe = 0.662459 eV
dEtot = 0.662459 eV
Count spin degeneration of 2:
dEh = 0 eV
dEe = 1.32492 eV
dEtot = 1.32492 eV

## Slide 16
Charge/dipole correction: Ideal
vasp_correction_charge-test.bat
python vasp_correction_charge.py .\Defect\ZnO\DOS 
Provide already-known dielectric constant 
python vasp_correction_charge.py .\Defect\ZnO\DOS 12.2
Output:
*** Read dielectric constant from argument [12.2]
eps(tot): 12.2
*** Read IDIPOL information from [.\Defect\ZnO\DOS\OUTCAR]
dipolemoment: [0.0, -0.0, -6.034717]
Tr[quadrupol] : -5.863427
Ecorr(di+quadrupol): -14.4355 eV
Ecorr(with field) : 0 eV
Ecorr(charge)=q^2 * aM / L : 0 eV
NELECT = 36.0
nVe = 36.0
q = 0.0
eps(tot)= 12.2 e0
L = 3.677614306961553 A
q^2 * aM : 0
(2/3) * q^2 * aM / L / eps(tot,av): 0 eV

## Slide 17
Charge/dipole correction: Ideal
vasp_correction_charge-test.bat
python vasp_correction_charge.py CAR_dir(IDIPOL) CAR_dir(Dielectric constant)
Provide CAR_dir for dielectric constant calculation
python vasp_correction_charge.py .\Defect\ZnO\DOS .\Defect\ZnO\Phonon
Output:
*** Read OUTCAR from [.\Defect\ZnO\Phonon\OUTCAR]
Information in OUTCAR:
ISPIN : 1
LEPSILON: T
e(tot): | 7.931 0 0|
| 0 7.931 0|
| -0 0 7.351|
trace average: 7.73768
e(ion): | 6.711 0 -7.6e-05|
| 0 6.711 -0.000116|
| -7.6e-05 -0.000116 7.868|
trace average: 7.09668
*** Read IDIPOL information from [.\Defect\ZnO\DOS\OUTCAR]
(cut here)
q = 0.0
eps(tot)= 7.737676333333333 e0
L = 3.677614306961553 A
q^2 * aM : 0
(2/3) * q^2 * aM / L / eps(tot,av): 0 eV

## Slide 18
Charge/dipole correction: VO+
vasp_correction_charge-test.bat
python vasp_correction_charge.py mode CAR_dir(IDIPOL) CAR_dir(Dielectric constant)
Provide CAR_dir for dielectric constant calculation
python vasp_correction_charge.py .\Defect\ZnO-VOp1\SCF .\Defect\ZnO\Phonon
Output:
*** Read OUTCAR from [.\Defect\ZnO\Phonon\OUTCAR]
Information in OUTCAR:
ISPIN : 1
LEPSILON: T
e(tot): | 7.931 0 0|
| 0 7.931 0|
| -0 0 7.351|
trace average: 7.73768
(cut)
*** Read IDIPOL information from [.\Defect\ZnO-VOp1\SCF\OUTCAR]
(cut)
Ecorr(charge)=q^2 * aM / L : 2.52695 eV
NELECT = 281.0
nVe = 282.0
q = 1.0
eps(tot)= 7.737676333333333 e0
L = 7.23325925567137 A
aM : 18.2781 eV*A
(2/3) * q^2 * aM / L / eps(tot,av): 0.217718 eV