## Slide 1
Defect calculation by VASP
Xinyi HE
2020.12.04

## Slide 2
How to get defect formation energy
1.How to get total energy of defect models
2.How to get chemical potential
Today’s contents

## Slide 3
How to get defect formation energy
Defect (D) formation energy:
Energy of defects cell
Energy of perfect cell
Correction Energy
Chemical potential
mel: Standard chemical potential
Dm: Chemical potential depend on growth condition
Valence band maximum

## Slide 4
Defect (D) formation energy:
Transition levels
Stable
Unstable
Fermi level
q=1+
q=2+
q=2-
q=1-
q=0
How to get defect formation energy

## Slide 5
How to get defect formation energy
Defect (D) formation energy:
Energy of defects cell
Energy of perfect cell
Valence band maximum
1. Calculate defect models

## Slide 6
How to get defect formation energy
Defect (D) formation energy:
Chemical potential
2. Calculate chemical potential window

## Slide 7
1.How to get total energy of defect models
Build a perfect supercell
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Relaxed perfect supercell
Build the defect models
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Get total energy EH
Get total energy Ed
Charged defect models
(changing NELECT in INCAR)
Relaxed defect models
Scf-consistent calculation by HSE06 hybrid functional
Get total energy Ed
Relaxed Charged defect models
Relax atomic positions (fixed cell) by GGA-PBE functional

## Slide 8
1.How to get total energy of defect models
Build a perfect supercell
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Relaxed perfect supercell
Build the defect models
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Get total energy EH
Get total energy Ed
Charged defect models
(changing NELECT in INCAR)
Relaxed defect models
Scf-consistent calculation by HSE06 hybrid functional
Get total energy Ed
Relaxed Charged defect models
Relax atomic positions (fixed cell) by GGA-PBE functional

## Slide 9
(1) How to build a perfect supercell
1. Get the relaxed cell [CONTCAR]
(4 atoms)
2. Build the supercell by vesta or p4vasp
Note: if it occurs errors when open CONTCAR in vesta, please rename CONTCAR to CONTCAR.vasp
ZnO
n×a  15 Å
a=b=3.3 Å
c=5.3 Å
4×4×3 supercell (192 atoms)
How to determine the supercell size
Open the relaxed ZnO primitive cell by vesta.
(Test energy VS supercell size)
Eg:

## Slide 10
1.How to get total energy of defect models
Build a perfect supercell
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Relaxed perfect supercell
Build the defect models
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Get total energy EH
Get total energy Ed
Charged defect models
(changing NELECT in INCAR)
Relaxed defect models
Scf-consistent calculation by HSE06 hybrid functional
Get total energy Ed
Relaxed Charged defect models
Relax atomic positions (fixed cell) by GGA-PBE functional

## Slide 11
(2) How to set input files for defect calculation
1. POSCAR
2. POTCAR
3. KPOINTS
K-Points
0
Gamma-centered
1 1 1
0 0 0
4. INCAR
Relaxation calculation by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
5. vasp-info
Get EH , ED , EV

## Slide 12
(2) How to set input files for defect calculation
4. INCAR
general:
System = xxx
ISTART = 0 ; ICHARG = 2
ENCUT = 500
ISMEAR = 0; SIGMA = 0.2
ISIF = 2
NSW = 100
IBRION = 2
EDIFF = 1E-4
EDIFFG = -0.03
LREAL= Auto
LCHARG = F
LWAVE = F
general:
System = xxx
ISTART = 0; ICHARG = 2
ENCUT = 400
ISMEAR = 0; SIGMA = 0.2
ISIF = 2
#NSW = 100
IBRION = -1
EDIFF = 1E-3
LREAL= Auto
LCHARG = F
LWAVE = F
ALGO = All
LHFCALC = .TRUE.
HFSCREEN = 0.2
PREC = Normal
Relaxation calculation by GGA-PBE functional
Scf-consistent calculation by HSE06 hybrid functional

## Slide 13
(2) How to set input files for defect calculation
5. vasp-info
#!/bin/bash
JOB_NAME=VC-S
NUM_NODE=2
NUM_CPU=14
TIME=23:30:00
#NODE_TYPE=s_core #MAX_CPU 1
#NODE_TYPE=q_core #MAX_CPU 4
#NODE_TYPE=f_node #MAX_CPU 28 MAX_NODE 2
NODE_TYPE=h_node #MAX_CPU 14
#NODE_TYPE=q_node #MAX_CPU 7
#BIN=vasp_ncl
#BIN=vasp_gpu
MAIL_TYPE=abe
MAIL_ADDR=h-xinyi@mces.titech.ac.jp
BIN=vasp_gam #vasp_std
LOG=vasp.log
GROUP=tgd-mts
BIN_DIR=/gs/hs0/tgd-mts/bin/
~
Gamma-only

## Slide 14
(2) How to set input files for defect calculation
Get EH, EV from the perfect supercell
grep ' without' OUTCAR |tail -n 1 | awk '{print $7}'
Get EH
python gbandedges
Get Ev
gbandedges in /gs/hs0/tgd-mts/Data
Efermi : 0.624
N band : 1036
N kpoint: 1
N spin : 1
Band gap: 2.403
Bottom of conduction band:
Energy : 1.993
K point: 1 ['0.1262379E-14', '0.1262379E-14', '0.1262379E-14']
Band : 865
Spin : 1
Top of valence band:
Energy : -0.410
K point: 1 ['0.1262379E-14', '0.1262379E-14', '0.1262379E-14']
Band : 864
Spin : 1
Ev

## Slide 15
1.How to get total energy of defect models
Build a perfect supercell
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Relaxed perfect supercell
Build the defect models
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Get total energy EH
Get total energy Ed
Charged defect models
(changing NELECT in INCAR)
Relaxed defect models
Scf-consistent calculation by HSE06 hybrid functional
Get total energy Ed
Relaxed Charged defect models
Relax atomic positions (fixed cell) by GGA-PBE functional

## Slide 16
(3) How to build defect models
Intrinsic point defects in ZnO:
Vacancy: VZn, VO
Substitution: ZnO, OZn
Interstitial: Zni, Oi
So, we need to build 6 defect models.
Open the relaxed ZnO perfect cell by vesta.

## Slide 17
(3) How to build defect models
Intrinsic point defects in ZnO:
Vacancy: VZn, VO
Substitution: ZnO, OZn
Interstitial: Zni, Oi
1
2
3
VZn

## Slide 18
(3) How to build defect models
Intrinsic point defects in ZnO:
Vacancy: VZn, VO
Substitution: ZnO, OZn
Interstitial: Zni, Oi
1
3
OZn
2. Change to O

## Slide 19
(3) How to build defect models
Intrinsic point defects in ZnO:
Vacancy: VZn, VO
Substitution: ZnO, OZn
Interstitial: Zni, Oi
1
OZn

## Slide 20
(3) How to build defect models
Intrinsic point defects in ZnO:
Vacancy: VZn, VO
Substitution: ZnO, OZn
Interstitial: Zni, Oi
2. Add interstitial O
Oi

## Slide 21
(3) How to build defect models
Intrinsic point defects in ZnO:
Vacancy: VZn, VO
Substitution: ZnO, OZn
Interstitial: Zni, Oi
2. Add interstitial O
Oi
3

## Slide 22
1.How to get total energy of defect models
Build a perfect supercell
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Relaxed perfect supercell
Build the defect models
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Get total energy EH
Get total energy Ed
Charged defect models
(changing NELECT in INCAR)
Relaxed defect models
Scf-consistent calculation by HSE06 hybrid functional
Get total energy Ed
Relaxed Charged defect models
Relax atomic positions (fixed cell) by GGA-PBE functional

## Slide 23
1.How to get total energy of defect models
Build a perfect supercell
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Relaxed perfect supercell
Build the defect models
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Get total energy EH
Get total energy Ed
Charged defect models
(changing NELECT in INCAR)
Relaxed defect models
Scf-consistent calculation by HSE06 hybrid functional
Get total energy Ed
Relaxed Charged defect models
Relax atomic positions (fixed cell) by GGA-PBE functional

## Slide 24
(4) How to set input files for charged defect
1. POSCAR
2. POTCAR
3. KPOINTS
K-Points
0
Gamma-centered
1 1 1
0 0 0
4. INCAR
Relaxation calculation
Scf-consistent calculation
Get ED
Change NELECT tag
Keep

## Slide 25
(4) How to set input files for charged defect
general:
System = xxx
NELECT =
ISTART = 0 ; ICHARG = 2
ENCUT = 500
ISMEAR = 0; SIGMA = 0.2
ISIF = 2
NSW = 100
IBRION = 2
EDIFF = 1E-4
EDIFFG = -0.03
LREAL= Auto
LCHARG = F
LWAVE = F
general:
System = xxx
NELECT =
ISTART = 0; ICHARG = 2
ENCUT = 400
ISMEAR = 0; SIGMA = 0.2
ISIF = 2
#NSW = 100
IBRION = -1
EDIFF = 1E-3
LREAL= Auto
LCHARG = F
LWAVE = F
ALGO = All
LHFCALC = .TRUE.
HFSCREEN = 0.2
PREC = Normal
Relaxation calculation by GGA-PBE functional
Scf-consistent calculation by HSE06 hybrid functional
4. INCAR for charged defect cells
Check NELECT from defect model calculation:
Eg: NELECT = 70; 1+ states: NELECT = 69; 1- states: NELECT = 71.
grep NELECT OUTCAR

## Slide 26
1.How to get total energy of defect models
Build a perfect supercell
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Relaxed perfect supercell
Build the defect models
Relax atomic positions (fixed cell) by GGA-PBE functional
Scf-consistent calculation by HSE06 functional
Get total energy EH Ev
Get total energy Ed
Charged defect models
(changing NELECT in INCAR)
Relaxed defect models
Scf-consistent calculation by HSE06 hybrid functional
Get total energy Ed
Relaxed Charged defect models
Relax atomic positions (fixed cell) by GGA-PBE functional

## Slide 27
(4) How to set input files for charged defect
Some errors may occur in the VASP calculation process
VERY BAD NEWS! internal error in subroutine INVGRP:
inverse of rotation matrix was not found (increase SYMPREC) 3
Set SYMPREC=1E-3 in INCAR

## Slide 28
How to get defect formation energy
Defect (D) formation energy:
Chemical potential
2. Calculate chemical potential window

## Slide 29
2.How to get chemical potential
(1) Condition for stable growth of ZnO
where < 0 and < 0
Chemical potential
mel: Standard chemical potential of elements  total energy eg: mZn=E(Zn)
Dm: Chemical potential depend on growth condition chemical potential window
Chemical potential window

## Slide 30
2.How to get chemical potential
(1) Condition for stable growth of SrTiO3
where < 0 < 0 and < 0
(2) Condition to avoid competing phases:
……
Chemical potential
mel: Standard chemical potential of elements  total energy eg: mZn=E(Zn)
Dm: Chemical potential depend on growth condition chemical potential window
Chemical potential window
Check in Materials Projects
Calculate the total energy of
elemental phases and competing phases

## Slide 31
2.How to get chemical potential
Calculate the total energy of
elemental phases and competing phases
Get chemical potential window by Chesta
Download Chesta in /gs/hs0/tgd-mts/Data
Open chemicalwindow-2e.xlsx in Chesta3.2.6.9 folder
データファイル作成ウィザード3.xls
Chesta3.exe

## Slide 32
How to get defect formation energy
Defect (D) formation energy:
Energy of defects cell
Energy of perfect cell
Correction Energy
Chemical potential
Valence band maximum
Use defect_anlysis.xlsx in in /gs/hs0/tgd-mts/Data

## Slide 33: 1. H, O, F doping-Interstitial sites
Summary
How to get defect formation energy
1.How to get total energy of defect models
2.How to get chemical potential
Energy of defects cell
Energy of perfect cell
Correction Energy
Chemical potential
Valence band maximum

## Slide 34
DFT calculation by VASP
Xinyi HE
2020.11.27

## Slide 35
The linux command
Change folders: cd
Rename folder/file names: mv
Copy files: cp
Copy folders recursively with tree: cp -r
Create folders: mkdir
Remove files: rm
Remove folders: rm -r
Show files in the current folder: ls
Edit a txt file: vi  a (append)  :wq(save the file) / :q!(not save and quit)

## Slide 36
The needed softwares
P4vasp:
Edit/show the crystal structures (POSCAR/CONTCAR)
Show DOS or band structures (vasprun.xml)
Use for example [p4v POSCAR; p4v vasprun.xml]
Vesta:
Edit/show the crystal structures (POSCAR/CONTCAR)
Change format .cif  .vasp
Use as [vesta POSCAR]

## Slide 37
The needed software
P4vasp:
Edit/show the crystal structures (POSCAR/CONTCAR)
Show DOS or band structures (vasprun.xml)
Use as [p4v POSCAR; p4v vasprun.xml]

## Slide 38
The needed software
In linux system:
Use as [vesta POSCAR]
vi ~/.bashrc
a
export VESTA=/gs/hs0/tgd-mts/VESTA-x86_64
export PATH="$PATH:$VESTA"
alias vesta='/gs/hs0/tgd-mts/VESTA-x86_64/VESTA’
(cat /gs/hs0/tgd-mts/Data/vesta-info)
:wq
chmod 777 -R /gs/hs0/tgd-mts/VESTA-x86_64/
vesta
In Windows system:
Download /gs/hs0/tgd-mts/Data/VESTA-win64
Enter VESTA-win64 and click VESTA.exe
Vesta:

## Slide 39
INCAR in POTCAR in KPOINTS in
POSCAR in
CHGCAR in/out WAVECAR in/out
IBZKPT out CONTCAR out
OUTCAR out CHG out EIGENVAL out DOSCAR out PROCAR out OSZICAR out PCDAT out XDATCAR out
Input/output files

## Slide 40
https://www.vasp.at/wiki/index.php/The_VASP_Manual
Input/output files

## Slide 41
https://www.vasp.at/wiki/index.php/The_VASP_Manual
Input/output files

## Slide 42
Input files
1. POSCAR: Crystal structure
2. POTCAR: Pseudopotential
3. KPOINTS: K-points
4. INCAR: Calculation setting
5. vasp-info: Submit script, called from qvasp

## Slide 43
Input files
POSCAR
The lattice constant and the atomic positions
POSCAR of ZnO:
Zn2 O2 # system information
1.0 # universal scaling parameters
3.2891025543 0.0000000000 0.0000000000 # lattice vector
-1.6445512772 2.8484463677 0.0000000000
0.0000000000 0.0000000000 5.3068208694
Zn O # elements
2 2 # number of atoms
Direct # positions in Fractional coordinates / if it’s Cartesian, it means Cartesian coordinates
0.333333340 0.666666681 0.000548000 # atomic position #Zn1
0.666666706 0.333333340 0.500548017 #Zn2
0.333333340 0.666666681 0.379761996 #O1
0.666666706 0.333333340 0.879761996 #O2

## Slide 44
Input files
POSCAR
The lattice constant and the atomic positions
POSCAR of ZnO:
Zn2 O2 # system information
1.0 # universal scaling parameters
3.2891025543 0.0000000000 0.0000000000 # lattice vector
-1.6445512772 2.8484463677 0.0000000000
0.0000000000 0.0000000000 5.3068208694
Zn O # elements
2 2 # number of atoms
Cartesian # positions in Cartesian coordinates
0.000000000 1.898964286 0.002908138 # atomic position #Zn1
1.644551396 0.949482143 2.656318665 #Zn2
0.000000000 1.898964286 2.015328884 #O1
1.644551396 0.949482143 4.668739319 #O2

## Slide 45
Input files
POSCAR
The lattice constant and the atomic positions
How to get POSCAR:
Get the experimental data and edit by self
(need the lattice constant and the atomic positions )
2. From database
(1) Materials Project https://materialsproject.org/
format transfer: cifvasp (by vesta)
(2) ICSD

## Slide 46
Input files
POSCAR
The lattice constant and the atomic positions
How to get POSCAR:
2. From database
(1) Materials Project https://materialsproject.org/
1
2
3

## Slide 47
Input files
POSCAR
The lattice constant and the atomic positions
How to get POSCAR:
2. From database
(1) Materials Project https://materialsproject.org/

## Slide 48
Input files
POSCAR
The lattice constant and the atomic positions
How to get POSCAR:
2. From database
(1) Materials Project https://materialsproject.org/

## Slide 49
Input files
POSCAR
The lattice constant and the atomic positions
How to get POSCAR:
2. From database
(1) Materials Project https://materialsproject.org/
Get cif file

## Slide 50
Input files
POSCAR
The lattice constant and the atomic positions
How to get POSCAR:
2. From database
(1) Materials Project https://materialsproject.org/
format transfer: cifvasp (by vesta)
vesta xx.cif or
Fileexport.vasp
1
2
3

## Slide 51
Input files
POTCAR
PAW_PBE Fe 06Sep2000
8.00000000000000000
parameters from PSCTR are:
VRHFIN =Fe: d7 s1
LEXCH = PE
EATOM = 594.4687 eV, 43.6922 Ry
TITLE = PAW_PBE Fe 06Sep2000
LULTRA = F use ultrasoft PP
IUNSCR = 1 unscreen: 0-lin 1-nonlin 2-no
RPACOR = 2.000 partial core radius
POMASS = 55.847; ZVAL = 8.000 mass and valenz
RCORE = 2.300 outmost cutoff radius
RWIGS = 2.460; RWIGS = 1.302 wigner-seitz radius (au A)
ENMAX = 267.883; ENMIN = 200.912 eV
RCLOC = 1.701 cutoff for local pot
LCOR = T correct aug charges
LPAW = T paw PP
EAUG = 511.368
…
VRHFIN: valence electron configuration
TITEL: which element
ZVAL: valence electron number
ENMAX: cutoff energy
The mass, valence, pseudopotential for each element.

## Slide 52
Input files
POTCAR
The mass, valence, pseudopotential for each element.
How to get POTCAR:
From POT folder: /pwd/= /gs/hs0/tgd-mts/POT/potpaw_PBE54/elements
cat /pwd/Zn/POTCAR /pwd/O/POTCAR > POTCAR
potcar.sh
(mkdir ~/bin; cp /gs/hs0/tgd-mts/Data/potcar.sh ~/bin; chmod u+x ~/bin/potcar.sh)
potcar.sh Zn O
grep TIT POTCAR
[he@csrv7 1-relax]$ grep TIT POTCAR
TITEL = PAW_PBE Zn 06Sep2000
TITEL = PAW_PBE O 08Apr2002

## Slide 53
Input files
POTCAR
The mass, valence, pseudopotential for each element.
How to get POTCAR:
For some elements, there are several POTCAR versions
Eg: cd /gs/hs0/tgd-mts/POT/potpaw_PBE54/elements/; ls Ti*
19D28063@login0:/gs/hs0/tgd-mts/Data> cd /gs/hs0/tgd-mts/POT/potpaw_PBE54/elements/
19D28063@login0:/gs/hs0/tgd-mts/POT/potpaw_PBE54/elements> ls Ti*
Ti:
POTCAR PSCTR
Ti_pv:
POTCAR PSCTR
Ti_sv:
POTCAR PSCTR
Ti_sv_GW:
POTCAR PSCTR
Recommended POTCAR: /gs/hs0/tgd-mts/Data/POTCAR.pdf
_pv and _sv: treat the p and s semi-core states as valence states
(i.e. for Ti_pv the 3p states are treated as valence states,
and for Ti_sv the 3s and 3p states are treated as valence states).
_d: treat the d semi core states as valence states
(i.e. for Ga d the 3d states are treated as valence states)

## Slide 54
Input files
KPOINTS
K-POINTS # Comment
0 # automatic generation of k-points
Gamma # gamma-centered
4 4 4 # grid 4x4x4
0 0 0 # shift (usually 0 0 0)
The Bloch vectors (k-points) that will be used to sample the Brillouin zone
KPOINTS for the DOS calculation: denser k-points

## Slide 55
Input files
KPOINTS
K-POINTS # Comment
0 # automatic generation of k-points
Gamma # gamma-centered
4 4 4 # grid 4x4x4
0 0 0 # shift (usually 0 0 0)
The Bloch vectors (k-points) that will be used to sample the Brillouin zone
kpoints.sh
(cp /gs/hs0/tgd-mts/Data/kpoints.sh ~/bin; chmod u+x ~/bin/kpoints.sh )
kpoints.sh 4 4 4
cat KPOINTS
19D28063@login0:/gs/hs0/tgd-mts/Data> kpoints.sh 4 4 4
19D28063@login0:/gs/hs0/tgd-mts/Data> cat KPOINTS
K-Points
0
Gamma-centered
4 4 4
0 0 0

## Slide 56
Input files
KPOINTS
The Bloch vectors (k-points) that will be used to sample the Brillouin zone
KPOINTS for the band structure calculation:
K-Path # comment
20 # 20 intersections, 20 k-points between two high symmetry points
Line-Mode # line mode to generate k-points
Reciprocal # reciprocal coordinates
0.0000000000 0.0000000000 0.0000000000 G # high symmetry point
0.0000000000 0.5000000000 0.0000000000 X # band along GX
0.0000000000 0.5000000000 0.0000000000 X
0.5000000000 0.5000000000 0.0000000000 M
0.5000000000 0.5000000000 0.0000000000 M
0.0000000000 0.0000000000 0.0000000000 G
0.0000000000 0.0000000000 0.0000000000 G
0.5000000000 0.5000000000 0.5000000000 R

## Slide 57
Input files
KPOINTS
The Bloch vectors (k-points) that will be used to sample the Brillouin zone
KPOINTS for the band structure calculation:
https://www.cryst.ehu.es/cgi-bin/cryst/programs/nph-kv-list
1. Input space group
2.Click

## Slide 58
Input files
KPOINTS
The Bloch vectors (k-points) that will be used to sample the Brillouin zone
KPOINTS for the band structure calculation:
https://www.cryst.ehu.es/cgi-bin/cryst/programs/nph-kv-list
Click

## Slide 59
Input files
KPOINTS
The Bloch vectors (k-points) that will be used to sample the Brillouin zone
KPOINTS for the band structure calculation:
https://www.cryst.ehu.es/cgi-bin/cryst/programs/nph-kv-list

## Slide 60
Input files
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 550
ISMEAR = 0
ISIF = 3
NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = F
LCHARG = F
OK to input “space” before or after “=”
eg: ISMEAR=0 and ISMEAR = 0 ----same
Don’t use “tab”，use “space”.

## Slide 61
System: what to calculate, can be random, no effect to the result
Input files
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 550
ISMEAR = 0 (SIGMA = 0.1)
ISIF = 3
NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = F
LCHARG = F

## Slide 62
ENCUT specifies the cutoff energy for the planewave basis set in eV. Default: ENCUT = largest ENMAX on the POTCAR file
(grep ENMAX POTCAR)
If ISIF=3 (relax the cell), ENCUT > 1.3* ENMAX
Input files
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 550
ISMEAR = 0
(SIGMA = 0.1)
ISIF = 3
NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = F
LCHARG = F
[he@csrv7 1-relax]$ grep ENMAX POTCAR
ENMAX = 276.723; ENMIN = 207.542 eV
ENMAX = 400.000; ENMIN = 300.000 eV

## Slide 63
ISMEAR: determines how the partial occupancies for each orbital.
For semiconductors or insulators with large kpoints: ISMEAR=-5 (tetrahedron method, more accurate for simple band structures For large supercells and Gamma-point only calc: ISMEAR=0 (Gaussian smearing)
For metals: ISMEAR=0 (Gaussian smearing) or 1
For DOS cal.: ISMEAR= -5 or 0
if k-points < 3, must use ISMEAR= 0
Input files
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 550
ISMEAR = 0
(SIGMA = 0.1)
ISIF = 3
NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = F
LCHARG = F

## Slide 64
ISIF: determines whether the stress tensor is calculated.
=3: relax the lattice constant and atomic positions
=2: only relax the atomic positions
Input files
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 550
ISMEAR = 0
ISIF = 3
NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = F
LCHARG = F

## Slide 65
NSW: the maximum number of ionic steps.
Input files
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 550
ISMEAR = 0
ISIF = 3
NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = F
LCHARG = F
ionic steps

## Slide 66
IBRION: how the ions are updated and moved.
IBRION=2
Input files
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 550
ISMEAR = 0
ISIF = 3
NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = F
LCHARG = F

## Slide 67
EDIFF: the global break condition for the electronic SC-loop.
Default: EDIFF = 1E-4
EDIFF = 1E-6
EDIFFG: the break condition for the ionic relaxation loop.
Default: EDIFFG = EDIFF×10
EDIFFG = -0.01 # this case the relaxation will stop if all forces are smaller than |EDIFFG| . This is usually a more convenient setting.
Input files
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 550
ISMEAR = 0
ISIF = 3
NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = F
LCHARG = F

## Slide 68
LWAVE: whether the wavefunctions are written to the WAVECAR file
LCHARG: whether the charge densities (CHGCAR and CHG) are written
Default: LWAVE=T; LCHARG=T
In order to save memory space, not write WAVECAR, CHGCAR and CHG
Input files
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 550
ISMEAR = 0
ISIF = 3
NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = F
LCHARG = F

## Slide 69
Input files
vasp-info
#!/bin/bash
JOB_NAME=VC-S
NUM_NODE=4
NUM_CPU=7
TIME=01:00:00
#NODE_TYPE=s_core #MAX_CPU 1
#NODE_TYPE=q_core #MAX_CPU 4
#NODE_TYPE=f_node #MAX_CPU 28 #NODE_TYPE=h_node #MAX_CPU 14
NODE_TYPE=q_node #MAX_CPU 7
#BIN=vasp_ncl
#BIN=vasp_gpu
MAIL_TYPE=abe
MAIL_ADDR=xx@mces.titech.ac.jp
BIN=vasp_std
LOG=vasp.log
GROUP=tgd-mts
BIN_DIR=/gs/hs0/tgd-mts/bin/
Use vasp by qvasp
qstate: check the task state
qdel: delete the task
cp /gs/hs0/tgd-mts/Data/vasp-info .

## Slide 70
Output files
1. CONTCAR: relaxed crystal structure
2. OUTCAR: detailed output of a VASP run

## Slide 71
Output files
CONTCAR
The lattice constant and the atomic positions
eg:
Zn2 O2 # system information
1.0 # universal scaling parameters
3.2891025543 0.0000000000 0.0000000000 # lattice vector
-1.6445512772 2.8484463677 0.0000000000
0.0000000000 0.0000000000 5.3068208694
Zn O # elements
2 2 # number of atoms
Direct # positions in Fractional coordinates / if it’s Cartesian, it means cartesian coordinates
0.333333340 0.666666681 0.000548000 # atomic position #Zn1
0.666666706 0.333333340 0.500548017 #Zn2
0.333333340 0.666666681 0.379761996 #O1
0.666666706 0.333333340 0.879761996 #O2

## Slide 72
Output files
OUTCAR
Detailed output of a VASP run:
A summary of the used input parameters.
The electronic steps, KS-eigenvalues.
Stress tensors.
Forces on the atoms.
Local charges and magnetic moments.
Dielectric properties
…
FREE ENERGIE OF THE ION-ELECTRON SYSTEM (eV)
---------------------------------------------------
free energy TOTEN = -39.74588443 eV
energy without entropy= -39.74588443 energy(sigma->0) = -39.74588443
Total CPU time used (sec): 4.879
User time (sec): 4.823
Energy:
Time:

## Slide 73
Output files
OUTCAR
FREE ENERGIE OF THE ION-ELECTRON SYSTEM (eV)
---------------------------------------------------
free energy TOTEN = -39.74588443 eV
energy without entropy= -39.74588443 energy(sigma->0) = -39.74588443
Total CPU time used (sec): 4.879
User time (sec): 4.823
Energy:
Time:
grep ' without' OUTCAR |tail -n 1 | awk '{print $7}'
grep "Total CPU time used (sec): " OUTCAR
[he@csrv7 scf]$ ti
Total CPU time used (sec): 4.879
[he@csrv7 scf]$ grep ' without' OUTCAR |tail -n 1 | awk '{print $7}'
-39.74588443

## Slide 74
Input files for band structures/DOS
1. POSCAR: Crystal structure
2. POTCAR: Pseudopotential
3. KPOINTS: K-points
4. INCAR: Calculation setting
5. vasp-info: Submit script
6. WAVECAR
7. CHGCAR

## Slide 75
ENCUT can be ENMAX, smaller than the relaxation process
Not change in the crystal structure
The wavefunctions are written to the WAVECAR file
The charge densities are written to CHGCAR and CHG file
Input files for scf calculation
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 400
ISMEAR = 0
#ISIF = 3
#NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = T
LCHARG = T

## Slide 76
ISTART = 1 : read WAVECAR
ICHARG = 11: read CHGCAR
LORBIT = 11: write projected wave function character of each orbital
Input files for band structures
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 400
ISMEAR = 0
#ISIF = 3
#NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = T
LCHARG = T
ISTART = 1
ICHARG = 11
LORBIT = 11

## Slide 77
Input files for DOS
INCAR
Tell VASP what to calculate and how to calculate
general:
System = ZnO
ENCUT = 400
ISMEAR = -5
#ISIF = 3
#NSW = 100
IBRION = 2
EDIFF = 1E-6
EDIFFG = -0.01
LWAVE = T
LCHARG = T
ISTART = 1
ICHARG = 11
LORBIT = 11
NEDOS = 801
ISTART = 1 : read WAVECAR
ICHARG = 11: read CHGCAR
LORBIT = 11: write projected wave function character of each orbital
ISMEAR = -5: more accurate for DOS calculation
NEDOS: number of gridpoints
Default: NEDOS = 301

## Slide 78
Exercise
cp –r /gs/hs0/tgd-mts/Data/ZnO .
Use ZnO as an example
19D28063@login0:/gs/hs0/tgd-mts/Data/ZnO> ls
1-relax 2-scf 3-band 4-dos exercise ZnO_mp-2133_primitive.cif ZnO_mp-2133_primitive.vasp
cd exercise; ls
19D28063@login0:/gs/hs0/tgd-mts/Data/ZnO> cd exercise
19D28063@login0:/gs/hs0/tgd-mts/Data/ZnO/exercise> ls
ZnO_mp-2133_primitive.cif ZnO_mp-2133_primitive.vasp
mkdir 1-relax 2-scf 3-band 4-dos
cd 1-relax; cp ../ZnO_mp-2133_primitive.vasp POSCAR; cat POSCAR
vi INCAR; cat INCAR
vi KPOINTS; (kpoints.sh 9 9 5) cat KPOINTS

## Slide 79
Exercise
Use ZnO as an example
POTCAR:
cat /pwd/Zn/POTCAR /pwd/O/POTCAR > POTCAR
/pwd/= /gs/hs0/tgd-mts/POT/potpaw_PBE54/elements
potcar.sh Zn O
grep TIT POTCAR
cp /gs/hs0/tgd-mts/Data/vasp-info .
vi vasp-info .  :wq
qvasp
grep ' without' OUTCAR |tail -n 1 | awk '{print $7}'
grep "Total CPU time used (sec): " OUTCAR
p4v CONTCAR
Check the results

## Slide 80: 1. H, O, F doping-Interstitial sites
Summary
Know how to set input files:
INCAR POTCAR KPOINTS POSCAR
How to check the results/output files:
CONTCAR OUTCAR
How to submit the task:
qvasp; qstate; qdel
How to use p4v, vesta