## Slide 1
Electronic structure: SnSe vs Sn(Se0.6Te0.4)
Direct
Indirect
Notes: Then I investigated the electronic structures. This is diffuse reflectance for pure tin selenide and x of 0.4. For both cases, indirect gap is smaller than direct gap, and the bandgap becomes smaller by tellurium doping. We can see clear band structure change in valence band region. Valence band maximum shifts to higher energy by tellurium doping. So, The contribution of tellurium orbital reduces the band gap.